Mortar is a workable paste used to bind construction blocks together and fill the gaps between them. The blocks may be stone, brick, cinder blocks, etc. Mortar becomes hard when it sets, resulting in a rigid aggregate structure. Modern mortars are typically made from a mixture of sand, a binder such as cement or lime, and water. Mortar can also be used to fix, or point, masonry when the original mortar has washed away.

In the most general sense of the word, a cement is a binder, a substance that sets and hardens independently, and can bind other materials together. The word "cement" traces to the Romans, who used the term opus caementicium to describe masonry resembling modern concrete that was made from crushed rock with burnt lime as binder. The volcanic ash and pulverized brick additives that were added to the burnt lime to obtain a hydraulic binder were later referred to as cementum, cimentum, cäment and cement.

Cement used in construction is characterized as hydraulic or non-hydraulic. Hydraulic cements (e.g., Portland cement) harden because of hydration chemical reactions that occur independently of the mixture's water content; they can harden even underwater or when constantly exposed to wet weather. The chemical reaction that results when the anhydrous cement powder is mixed with water produces hydrates that are not water-soluble. Non-hydraulic cements (e.g., lime and gypsum plaster) must be kept dry in order to retain their strength.

The most important use of cement is the production of mortar and concrete—the bonding of natural or artificial aggregates to form a strong building material that is durable in the face of normal environmental effects.

Concrete should not be confused with cement because the term cement refers to the material used to bind the aggregate materials of concrete. Concrete is a combination of a cement and aggregate.

Construction aggregate, or simply "aggregate", is a broad category of coarse particulate material used in construction, including sand, gravel, crushed stone, slag, recycled concrete and geosynthetic aggregates. Aggregates are a component of composite materials such as concrete and asphalt concrete; the aggregate serves as reinforcement to add strength to the overall composite material. Due to the relatively high hydraulic conductivity value as compared to most soils, aggregates are widely used in drainage applications such as foundation and French drains, septic drain fields, retaining wall drains, and road side edge drains. Aggregates are also used as base material under foundations, roads, and railroads. To put it another way, aggregates are used as a stable foundation or road/rail base with predictable, uniform properties (e.g. to help prevent differential settling under the road or building), or as a low-cost extender that binds with more expensive cement or asphalt to form concrete.

Lime is a general term for calcium-containing inorganic materials, in which carbonates, oxides and hydroxides predominate. Strictly speaking, lime is calcium oxide or calcium hydroxide. It is also the name for a single mineral (native lime) of the CaO composition, occurring very rarely.[citation needed] The word 'lime' originates with its earliest use as building mortar and has the sense of 'sticking or adhering'.[1] Lime can also refer to a sticky substance (birdlime) smeared on branches to catch small birds.

These materials are still used in large quantities as building and engineering materials (including limestone products, concrete and mortar) and as chemical feedstocks, among other uses. Lime industries and the use of many of the resulting products date from prehistoric periods in both the Old World and the New World.

The rocks and minerals from which these materials are derived, typically limestone or chalk, are composed primarily of calcium carbonate. They may be cut, crushed or pulverized and chemically altered. "Burning" (calcination) converts them into the highly caustic material quicklime (calcium oxide, CaO) and, through subsequent addition of water, into the less caustic (but still strongly alkaline) slaked lime or hydrated lime (calcium hydroxide, Ca(OH)2), the process of which is called slaking of lime.

When the term is encountered in an agricultural context, it probably refers to agricultural lime. Otherwise it most commonly means slaked lime, as the more dangerous form is usually described more specifically as quicklime or burnt lime.

## Lime production process

- Limestone is extracted from quarries or mines.

- Part of the extracted stone, selected according to its chemical composition and granulometry, is calcinated at about 1000°C in different types of kiln, fired by such fuels as natural gas, coal, fuel oil, lignite, etc.

Quicklime is produced according to the reaction: CaCO3 + heat → CaO + CO2

- Quicklime can be hydrated, i.e., combined with water.

Slaked Lime Calcium hydroxide Ca(OH)2 Hydrated lime is produced according to the reaction:

CaO + H2O --> Ca(OH)2

Cement

In the most general sense of the word, a cement is a binder, a substance that sets and hardens independently, and can bind other materials together. The word "cement" traces to the Romans, who used the term opus caementicium to describe masonry resembling modern concrete that was made from crushed rock with burnt lime as binder. The volcanic ash and pulverized brick additives that were added to the burnt lime to obtain a hydraulic binder were later referred to as cementum, cimentum, cäment and cement.

Cement used in construction is characterized as hydraulic or non-hydraulic. Hydraulic cements (e.g., Portland cement) harden because of hydration chemical reactions that occur independently of the mixture's water content; they can harden even underwater or when constantly exposed to wet weather. The chemical reaction that results when the anhydrous cement powder is mixed with water produces hydrates that are not water-soluble. Non-hydraulic cements (e.g., lime and gypsum plaster) must be kept dry in order to retain their strength.

The most important use of cement is the production of mortar and concrete—the bonding of natural or artificial aggregates to form a strong building material that is durable in the face of normal environmental effects.

Concrete should not be confused with cement because the term cement refers to the material used to bind the aggregate materials of concrete. Concrete is a combination of a cement and aggregate.

In the manufacture of Portland cement, clinker is lumps or nodules, usually 3-25 mm in diameter, produced by sintering limestone and alumino-silicate during the cement kiln stage.

Sintering is a method for making objects from powder, by heating the material in a sintering furnace[1] below its melting point (solid state sintering) until its particles adhere to each other. Sintering is traditionally used for manufacturing ceramic objects

## History of the origin of cement

## Early Uses

It is uncertain where it was first discovered that a combination of hydrated non-hydraulic lime and a pozzolan produces a hydraulic mixture (see also: Pozzolanic reaction), but concrete made from such mixtures was first used on a large scale by Roman engineers.[1] They used both natural pozzolans (trass or pumice) and artificial pozzolans (ground brick or pottery) in these concretes. Many excellent examples of structures made from these concretes are still standing, notably the huge monolithic dome of the Pantheon in Rome and the massive Baths of Caracalla.[2] The vast system of Roman aqueducts also made extensive use of hydraulic cement.[3]

Although any preservation of this knowledge in literary sources from the Middle Ages is unknown, medieval masons and some military engineers maintained an active tradition of using hydraulic cement in structures such as canals, fortresses, harbors, and shipbuilding facilities.[4][5] The technical knowledge of making hydraulic cement was later formalized by French and British engineers in the 18th century.[4]

A number of environmentally friendly initiatives for making the production of cement are significantly more efficient (10-40%) than current processes, namely the Kalina process initiated by Seimens.

### Modern cement

Modern hydraulic cements began to be developed from the start of the Industrial Revolution (around 1800), driven by three main needs:

- Hydraulic render (stucco) for finishing brick buildings in wet climates.

- Hydraulic mortars for masonry construction of harbor works, etc., in contact with sea water.

- Development of strong concretes.

In Britain particularly, good quality building stone became ever more expensive during a period of rapid growth, and it became a common practice to construct prestige buildings from the new industrial bricks, and to finish them with a stucco to imitate stone. Hydraulic limes were favored for this, but the need for a fast set time encouraged the development of new cements. Most famous was Parker's "Roman cement".[6] This was developed by James Parker in the 1780s, and finally patented in 1796. It was, in fact, nothing like any material used by the Romans, but was a "Natural cement" made by burning septaria - nodules that are found in certain clay deposits, and that contain both clay minerals and calcium carbonate. The burnt nodules were ground to a fine powder. This product, made into a mortar with sand, set in 5–15 minutes. The success of "Roman Cement" led other manufacturers to develop rival products by burning artificial mixtures of clay and chalk.

John Smeaton made an important contribution to the development of cements when he was planning the construction of the third Eddystone Lighthouse (1755-9) in the English Channel. He needed a hydraulic mortar that would set and develop some strength in the twelve hour period between successive high tides. He performed an exhaustive market research on the available hydraulic limes, visiting their production sites, and noted that the "hydraulicity" of the lime was directly related to the clay content of the limestone from which it was made. Smeaton was a civil engineer by profession, and took the idea no further. Apparently unaware of Smeaton's work, the same principle was identified by Louis Vicat in the first decade of the nineteenth century. Vicat went on to devise a method of combining chalk and clay into an intimate mixture, and, burning this, produced an "artificial cement" in 1817. James Frost,[7] working in Britain, produced what he called "British cement" in a similar manner around the same time, but did not obtain a patent until 1822. In 1824, Joseph Aspdin patented a similar material, which he called Portland cement, because the render made from it was in color similar to the prestigious Portland stone.

All the above products could not compete with lime/pozzolan concretes because of fast-setting (giving insufficient time for placement) and low early strengths (requiring a delay of many weeks before formwork could be removed). Hydraulic limes, "natural" cements, and "artificial" cements all rely upon their belite content for strength development. Belite develops strength slowly. Because they were burned at temperatures below 1250 °C, they contained no alite, which is responsible for early strength in modern cements. The first cement to consistently contain alite was made by Joseph Aspdin's son William in the early 1840s. This was what we call today "modern" Portland cement. Because of the air of mystery with which William Aspdin surrounded his product, others (e.g., Vicat and I.C. Johnson) have claimed precedence in this invention, but recent analysis[8] of both his concrete and raw cement have shown that William Aspdin's product made at Northfleet, Kent was a true alite-based cement. However, Aspdin's methods were "rule-of-thumb": Vicat is responsible for establishing the chemical basis of these cements, and Johnson established the importance of sintering the mix in the kiln.

William Aspdin's innovation was counterintuitive for manufacturers of "artificial cements", because they required more lime in the mix (a problem for his father), a much higher kiln temperature (and therefore more fuel), and the resulting clinker was very hard and rapidly wore down the millstones, which were the only available grinding technology of the time. Manufacturing costs were therefore considerably higher, but the product set reasonably slowly and developed strength quickly, thus opening up a market for use in concrete. The use of concrete in construction grew rapidly from 1850 onwards, and was soon the dominant use for cements. Thus Portland cement began its predominant role.

In the US the first large scale use of cement was Rosendale cement a natural cement mined from a massive deposit of a large dolostone rock deposit discovered in the early 19th century near Rosendale, New York. Rosendale cement was extremely popular for the foundation of buildings (e.g., Statue of Liberty, Capitol Building, Brooklyn Bridge) and lining water pipes. But it long curing time of at least a month made it unpopular after World War One in the construction of highways and bridges and many states and construction firms turned to the use of Portland Cement. Because of the switch to Portland Cement, by the end of the 1920s of the 15 Rosendale cement companies, only one had survived. But in the early 1930s it was soon discovered that Portland Cement while it had a faster setting time was not as durable, especially for highways, to the point that some states stop building highways and roads with cement. An engineer, Bertrain H. Wait, whose company had worked on the construction of the New York Cities Catskill Aqueduct, and was impressed with the durability of Rosendale cement, came up with a blend of both Rosendale and synthetic cements which has the good attributes of both: it was highly durable and had a much faster setting time. Mr. Wait convinced the New York Commissioner of Highways to construct an experimental section highway near New Paltz, New York, of one sack of Rosendale to six sacks of synthetic cement, and it was proved a success and for decades hence the Rosendale-synthetic cement blend became common use in highway and bridge construction. [9]

## Types of modern cement

### Portland cement

Cement is made by heating limestone (calcium carbonate), with small quantities of other materials (such as clay) to 1450 °C in a kiln, in a process known as calcination, whereby a molecule of carbon dioxide is liberated from the calcium carbonate to form calcium oxide, or quicklime, which is then blended with the other materials that have been included in the mix . The resulting hard substance, called 'clinker', is then ground with a small amount of gypsum into a powder to make 'Ordinary Portland Cement', the most commonly used type of cement (often referred to as OPC).

Portland cement is a basic ingredient of concrete, mortar and most non-speciality grout. The most common use for Portland cement is in the production of concrete. Concrete is a composite material consisting of aggregate (gravel and sand), cement, and water. As a construction material, concrete can be cast in almost any shape desired, and once hardened, can become a structural (load bearing) element. Portland cement may be grey or white.

### Portland cement blends

Portland cement blends are often available as inter-ground mixtures from cement manufacturers, but similar formulations are often also mixed from the ground components at the concrete mixing plant.[10]

Portland blastfurnace cement contains up to 70 % ground granulated blast furnace slag, with the rest Portland clinker and a little gypsum. All compositions produce high ultimate strength, but as slag content is increased, early strength is reduced, while sulfate resistance increases and heat evolution diminishes. Used as an economic alternative to Portland sulfate-resisting and low-heat cements.[11]

Portland flyash cement contains up to 30 % fly ash. The fly ash is pozzolanic, so that ultimate strength is maintained. Because fly ash addition allows a lower concrete water content, early strength can also be maintained. Where good quality cheap fly ash is available, this can be an economic alternative to ordinary Portland cement.[12]

Portland pozzolan cement includes fly ash cement, since fly ash is a pozzolan, but also includes cements made from other natural or artificial pozzolans. In countries where volcanic ashes are available (e.g. Italy, Chile, Mexico, the Philippines) these cements are often the most common form in use.

Portland silica fume cement. Addition of silica fume can yield exceptionally high strengths, and cements containing 5-20 % silica fume are occasionally produced. However, silica fume is more usually added to Portland cement at the concrete mixer.[13]

Masonry cements are used for preparing bricklaying mortars and stuccos, and must not be used in concrete. They are usually complex proprietary formulations containing Portland clinker and a number of other ingredients that may include limestone, hydrated lime, air entrainers, retarders, waterproofers and coloring agents. They are formulated to yield workable mortars that allow rapid and consistent masonry work. Subtle variations of Masonry cement in the US are Plastic Cements and Stucco Cements. These are designed to produce controlled bond with masonry blocks.

Expansive cements contain, in addition to Portland clinker, expansive clinkers (usually sulfoaluminate clinkers), and are designed to offset the effects of drying shrinkage that is normally encountered with hydraulic cements. This allows large floor slabs (up to 60 m square) to be prepared without contraction joints.

White blended cements may be made using white clinker and white supplementary materials such as high-purity metakaolin.

Colored cements are used for decorative purposes. In some standards, the addition of pigments to produce "colored Portland cement" is allowed. In other standards (e.g. ASTM), pigments are not allowed constituents of Portland cement, and colored cements are sold as "blended hydraulic cements".

Very finely ground cements are made from mixtures of cement with sand or with slag or other pozzolan type minerals that are extremely finely ground together. Such cements can have the same physical characteristics as normal cement but with 50% less cement particularly due to their increased surface area for the chemical reaction. Even with intensive grinding they can use up to 50% less energy to fabricate than ordinary Portland cements.[14]

### Non-Portland hydraulic cements

Pozzolan-lime cements. Mixtures of ground pozzolan and lime are the cements used by the Romans, and can be found in Roman structures still standing (e.g. the Pantheon in Rome). They develop strength slowly, but their ultimate strength can be very high. The hydration products that produce strength are essentially the same as those produced by Portland cement.

Slag-lime cements. Ground granulated blast furnace slag is not hydraulic on its own, but is "activated" by addition of alkalis, most economically using lime. They are similar to pozzolan lime cements in their properties. Only granulated slag (i.e. water-quenched, glassy slag) is effective as a cement component.

Supersulfated cements. These contain about 80% ground granulated blast furnace slag, 15 % gypsum or anhydrite and a little Portland clinker or lime as an activator. They produce strength by formation of ettringite, with strength growth similar to a slow Portland cement. They exhibit good resistance to aggressive agents, including sulfate.

Calcium aluminate cements are hydraulic cements made primarily from limestone and bauxite. The active ingredients are monocalcium aluminate CaAl2O4 (CaO · Al2O3 or CA in Cement chemist notation, CCN) and mayenite Ca12Al14O33 (12 CaO · 7 Al2O3 , or C12A7 in CCN). Strength forms by hydration to calcium aluminate hydrates. They are well-adapted for use in refractory (high-temperature resistant) concretes, e.g. for furnace linings.

Calcium sulfoaluminate cements are made from clinkers that include ye'elimite (Ca4(AlO2)6SO4 or C4A3 in Cement chemist's notation) as a primary phase. They are used in expansive cements, in ultra-high early strength cements, and in "low-energy" cements. Hydration produces ettringite, and specialized physical properties (such as expansion or rapid reaction) are obtained by adjustment of the availability of calcium and sulfate ions. Their use as a low-energy alternative to Portland cement has been pioneered in China, where several million tonnes per year are produced.[15][16] Energy requirements are lower because of the lower kiln temperatures required for reaction, and the lower amount of limestone (which must be endothermically decarbonated) in the mix. In addition, the lower limestone content and lower fuel consumption leads to a CO2 emission around half that associated with Portland clinker. However, SO2 emissions are usually significantly higher.

"Natural" cements correspond to certain cements of the pre-Portland era, produced by burning argillaceous limestones at moderate temperatures. The level of clay components in the limestone (around 30-35 %) is such that large amounts of belite (the low-early strength, high-late strength mineral in Portland cement) are formed without the formation of excessive amounts of free lime. As with any natural material, such cements have highly variable properties.

Geopolymer cements are made from mixtures of water-soluble alkali metal silicates and aluminosilicate mineral powders such as fly ash and metakaolin.

## The setting of cement

Cement sets when mixed with water by way of a complex series of hydration chemical reactions still only partly understood. The different constituents slowly hydrate and crystallise while the interlocking of their crystals gives to cement its strength. After the initial setting, immersion in warm water will speed up setting. In Portland cement, gypsum is added as a compound preventing cement flash setting. The time it takes for cement to set varies; and can take anywhere from twenty minutes for initial set, to twenty-four hours, or more, for final set.

## Environmental impacts

Cement manufacture causes environmental impacts at all stages of the process. These include emissions of airborne pollution in the form of dust, gases, noise and vibration when operating machinery and during blasting in quarries, and damage to countryside from quarrying. Equipment to reduce dust emissions during quarrying and manufacture of cement is widely used, and equipment to trap and separate exhaust gases are coming into increased use. Environmental protection also includes the re-integration of quarries into the countryside after they have been closed down by returning them to nature or re-cultivating them.

### CO2 emissions

Cement manufacturing releases CO2 in the atmosphere both directly when calcium carbonate is heated, producing lime and carbon dioxide,[17] and also indirectly through the use of energy if its production involves the emission of CO2. The cement industry is the second largest CO2 emitting industry behind power generation. The cement industry produces about 5% of global man-made CO2 emissions, of which 50% is from the chemical process, and 40% from burning fuel.[18] The amount of CO2 emitted by the cement industry is nearly 900 kg of CO2 for every 1000 kg of cement produced. [19]

In certain applications, lime mortar, reabsorbs the same amount of CO2 as was released in its manufacture, and has a lower energy requirement in production than mainstream cement. Newly developed cement types from Novacem[20] and Eco-cement can absorb carbon dioxide from ambient air during hardening.[21]

## Ancient mortar

The first mortars were made of mud and clay. Because of a lack of stone and an abundance of clay, Babylonian constructions were of baked brick, using lime or pitch for mortar. According to Roman Ghirshman, the first evidence of humans using a form of mortar was at the ziggurat of Sialk in Iran, built of sun-dried bricks in 2900 BC.[2] The Chogha Zanbil Temple in Iran was built in about 1250 BC with kiln-fired bricks and a strong mortar of bitumen.

In early Egyptian pyramids constructed about 2600–2500 BC, the limestone blocks were bound by mortar of mud and clay, or clay and sand.[3] In later Egyptian pyramids, the mortar was made of either gypsum or lime.[4] Gypsum mortar was essentially a mixture of plaster and sand and was quite soft.

Historically, building with concrete and mortar next appeared in Greece. The excavation of the underground aqueduct of Megara revealed that a reservoir was coated with a pozzolanic mortar 12 mm thick. This aqueduct dates back to c. 500 BC.[5] Pozzolanic mortar is a lime based mortar, but is made with an additive of volcanic ash that allows it to be hardened underwater; thus it is known as hydraulic cement. The Greeks obtained the volcanic ash from the Greek islands Thira and Nisiros, or from the then Greek colony of Dicaearchia (Pozzuoli) near Naples, Italy. The Romans later improved the use and methods of making what became known as pozzolanic mortar and cement.[4] Even later, the Romans used a mortar without pozzolana using crushed terra cotta, introducing aluminum oxide and silicon dioxide into the mix. This mortar was not as strong as pozzolanic mortar, but, because it was denser, it better resisted penetration by water.[6]

Hydraulic mortar was not available in ancient China, possibly due to a lack of volcanic ash. Around CE 500, sticky rice soup was mixed with slaked lime to make an inorganic−organic composite mortar that had more strength and water resistance than lime mortar. [7][8]

It is not understood why the art of making hydraulic mortar and cement, which was perfected and in such widespread use by both the Greeks and Romans, was then lost for almost two millennia. During the Middle Ages when the Gothic cathedrals were being built, the only active ingredient in the mortar was lime. Since cured lime mortar can be degraded by contact with water, many structures suffered from wind blown rain over the centuries.

Laying bricks with portland cement mortar

## Portland cement mortar

Portland cement mortar (often known simply as cement mortar) is created by mixing Ordinary Portland cement (OPC) with sand and water.

It was invented in 1794 by Joseph Aspdin and patented on 18 December 1824, largely as a result of various scientific efforts to develop stronger mortars than existed at the time. It was popularized during the late nineteenth century, and owing to the First World War, by 1930 it had superseded lime mortar for new construction. The main reasons for this were that Portland cement sets hard and quickly, allowing a faster pace of construction, and requires less skilled workers. However, as a general rule, Portland cement should not be used for the repair of older buildings constructed in lime mortar, which require the flexibility, softness and breathability of lime if they are to function correctly.

## Polymer cement mortar

Polymer cement mortars (PCM) are the materials which are made by partially replacing the cement hydrate binders of conventional cement mortar with polymers. The polymeric admixtures include latexes or emulsions, redispersible polymer powders, water-soluble polymers, liquid resins and monomers. It has low permeability, and it reduces the incidence of drying shrinkage cracking, mainly designed for repairing concrete structures. For an example see MagneLine.

## Lime mortar

Main article: Lime mortar

The speed of set can be increased by using impure limestones in the kiln, to form a hydraulic lime that will set on contact with water. Such a lime must be stored as a dry powder. Alternatively, a pozzolanic material such as calcined clay or brick dust may be added to the mortar mix. This will have a similar effect of making the mortar set reasonably quickly by reaction with the water in the mortar.

Using Portland cement mortars in repairs to older buildings originally constructed using lime mortar can be problematic. This is because lime mortar is softer than cement mortar, allowing brickwork a certain degree of flexibility to move to adapt to shifting ground or other changing conditions. Cement mortar is harder and allows less flexibility. The contrast can cause brickwork to crack where the two mortars are present in a single wall.

Lime mortar is considered breathable in that it will allow moisture to freely move through it and evaporate from its surface. In old buildings with walls that shift over time, there are often cracks which allow rain water into the structure. The lime mortar allows this moisture to escape through evaporation and keeps the wall dry. Repointing or rendering an old wall with cement mortar stops this evaporation and can cause problems associated with moisture behind the cement.

## Pozzolana mortar

Main article: Pozzolana

Pozzolana is a fine, sandy volcanic ash, originally discovered and dug in Italy at Pozzuoli in the region around Mount Vesuvius, but later at a number of other sites. The ancient Roman architect Vitruvius speaks of four types of pozzolana. It is found in all the volcanic areas of Italy in various colours: black, white, grey and red.

Finely ground and mixed with lime it acts like Portland cement and makes a strong mortar that will also set under water.